Certificate of Analysis

General properties:

Name： PDLLA5000-PEG5000-COOH

Molecular Weight： PEG MW:5000  PDLLA MW:5000

Cat.#： R-1056-55K

Lot.#： RP0162761

Manufacture Date： 2016.06.27

Date of Analysis： 2016.06.27

Recommended Retest date： 2017.06.27

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Off-white solid | White solid |
| 1H NMR | Identical to the structure | Identical to the structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 90% |

Report Date: 2016.06.27

This product is for research use only, Not for human or animal use